## Slide 1: Ab initio study for electron-phonon coupling of Nb-doped SrTiO3 with Jellium model
Minwoo Park and Suk Bum Chung
Department of Physics, University of Seoul

## Slide 2: Density Functional Theory
H : Hamiltonian, K : kinetic energy,
V : potential energy by charged nuclei,
U : the electron-electron interaction energy
: electrons density, : orbital
Many-body
One-body
K : Sham kinetic energy, Ven : electron-nuclei potential,
VH : Hartree (Coulomb) potential,
VXC : exchange-correlation potential

## Slide 3: DFT examples
Z2 in new 2D carbon systems
Raman shift of IV-VI 2D materials
Minwoo Park, el al., npj Computational Materials 4, 54 (2018)
Minwoo Park, et al. Scientific Reports 9, 19826 (2019)

## Slide 4: Superconductivity with BCS pairing
Bardeen-Cooper-Schrieffer (BCS) solution
  Assumes weak electron-phonon coupling and ‘adiabatic condition’ EF>>ħωD
  No pseudo-gap, i.e. nonzero ∆(T) only below Tc
  BCS ratio 2∆(T=0)/kBTc = 3.53
  Infinitesimal interaction sufficient, i.e. ∆(T=0)=2ħωDe-1/λ (λ: interaction parameter)
Under ‘adiabatic condition’ EF>>ħωD, solution found for large λ, i.e. strong interaction (Migdal-Eliashberg)

## Slide 5: Introduction of SrTiO3 (STO)
Cubic Perovskite
Wide indirect bandgap (3.25 eV)
Superconducting dome by doping
  n-type doping with Tc ≤ 0.3 K
Unconventional superconductor
  Not BCS – semiconductor, not metal
The origin of superconductivity is still open problem.
Structure of SrTiO3. The red spheres are oxygens, blue are Ti4+ cations, and the green ones are Sr2+.
M.N. Gastiasoro et al., Ann. Phys. (2020)

## Slide 6: Superconductivity in doped STO
● Superconducting dome over
finite range of doping discovered in
1960s!
● For half-a-century, the worst known
violation of EF>>ħωD
⇒ ┌ anything conventional left?
└ what about ∆(T=0)?
(Schooley et al Phys Rev Lett 1964;
Koonce et al Phys Rev 1967)

## Slide 7: Varieties in n-type STO
● Various methods, i.e. ┌ Nb substituting Ti
├ O vacancy
└ La substituting Sr
● Experimental probe easiest for Nb-doped STO
● Effect on TO1 mode may be dependent on dopant type
▶ Nearly identical hardening for Nb-doping and O-deficiency
→ higher dopant concentration means further from crystal quantum criticality
▶ No hardening confirmed for La-doping
(Bäuerle et al 1980 Z Phys B
Van Mechelen et al 2008 Phys Rev Lett)

## Slide 8: Difference with O-reduced STO
● Superconducting dome at lower density
observed in O-reduced STO
● BCS ratio NOT confirmed for O-reduced STO
- resistant to tunneling spectroscopy
(X Lin, Behnia et al. 2014 Phys Rev Lett)

## Slide 9: Tunneling spectroscopy on SrTi1-xNbxO3
X=0.005
(H Yoon, SB Chung, H Hwang et al. arXiv 2021)
● Cooper pair binding energy 2∆(T) measured by planar tunneling spectroscopy,
e.g. voltage difference between two di/dv peaks for very low T

## Slide 10: Measured gap to Tc ratio
▶ No pseudogap!
i.e. ∆(T)≠0
requires T<Tc
● BCS 2∆(T=0)/kBTc= 3.53 always holds!
⇒ conventional relation between the Cooper pair binding energy and Tc while EF<ħωD?
● Combine ∆(T) from tunneling spectroscopy with Tc from resistivity measurement
(H Yoon, SB Chung, H Hwang et al. arXiv 2021)

## Slide 11: Possible to bring back adiabaticity
Only TO1 mode remains slower than EF over the entire superconducting dome
Adiabatic condition would hold for pairing mediated only by TO1 mode
Explains the superconducting dome from
A. I. Lebedev, Phys. Solid State (2009)
TO1
EF
Underdoping – DOS too low
Overdoping – TO1 mode too hard

## Slide 12: Different phonon mediated interaction
● Conventional phonons:
→ couples to density
● TO1 phonons:
→ Rashba coupling to
spin current density
▶ TO1 phonons can also mediate pairing interaction
(Kozii and Fu PRL 2015; Y Wang et al. PRB 2016;
M Lee, H J Lee, J H Lee, SBC PRM 2020)
▶ Superconducting dome reproduced
(Y Yu, H Hwang, S Raghu, SBC arXiv 2021)

## Slide 13: To describe doping effect
Doping for SrTi1-xNbxO3
  n = 1019 – 1021 cm-3
  x = 10-3 –
Too big unit-cell
Size effect
- Nb doping is approximated with Jellium

## Slide 14: Introduction of Jellium model
Jellium
  - homogeneous background charge
  - uniformly distributed positive charges in space
Hel : kinetic and electron-electron repulsion
Hback : electrostatic interaction of the positive charge itself
Hel-back : electrostatic interaction of electron-background
TB parameters fitting
……
Phonon with Jel.
Get eigenvector (uTO1)
DFT band with uTO1 & Jel.
Procedure

## Slide 15: Phonon with Jellium for SrTi1-xNbxO3
(Negative frequency is imaginary value)
SrTi1-xNbxO3 |  | Frequency |  | Phonon eigenvector |  |  |  | 
x | ~n(cm^-3) | freq(THz) | freq(meV) | Sr | Ti | O' | O | O
0 | 0.00E+00 | -2.0208 | -8.357231 | 0.2544 | 0.4547 | -0.4578 | -0.5094 | -0.5094
0.000156 | 2.55E+18 | -2.0101 | -8.313077 | 0.2547 | 0.4542 | -0.4576 | -0.5096 | -0.5096
0.001563 | 2.55E+19 | -1.8818 | -7.782295 | 0.2576 | 0.4466 | -0.4643 | -0.5093 | -0.5093
0.003125 | 5.10E+19 | -1.7299 | -7.154136 | 0.2597 | 0.4370 | -0.4693 | -0.5106 | -0.5106
0.007813 | 1.27E+20 | -1.1799 | -4.879746 | 0.2495 | 0.3928 | -0.4708 | -0.5300 | -0.5300
0.015625 | 2.55E+20 | -0.0993 | -0.410523 | 0.6592 | 0.4702 | -0.3363 | -0.3401 | -0.3401
0.03125 | 5.10E+20 | 2.2935 | 9.4853147 | 0.4320 | 0.2989 | -0.5157 | -0.4786 | -0.4786
0.125 | 2.04E+21 | 6.7076 | 27.740514 | -0.2461 | 0.8303 | -0.2066 | -0.322 | -0.322
 | SrTi1-xNbxO3 |  |  |  | Phonon eigenvector |  |  |  | 
elect | x | ~n(cm^-3) | freq(THz) | freq(meV) | Sr | Ti | O' | O | O
0 | 0 | 0.00E+00 | -2.0208 | -8.357231 | 0.2544 | 0.4547 | -0.4578 | -0.5094 | -0.5094
0.01 | 0.000156 | 2.55E+18 | -2.0101 | -8.313077 | 0.2547 | 0.4542 | -0.4576 | -0.5096 | -0.5096
0.1 | 0.001563 | 2.55E+19 | -1.8818 | -7.782295 | 0.2576 | 0.4466 | -0.4643 | -0.5093 | -0.5093
0.2 | 0.003125 | 5.10E+19 | -1.7299 | -7.154136 | 0.2597 | 0.4370 | -0.4693 | -0.5106 | -0.5106
0.5 | 0.007813 | 1.27E+20 | -1.1799 | -4.879746 | 0.2495 | 0.3928 | -0.4708 | -0.5300 | -0.5300
1 | 0.015625 | 2.55E+20 | -0.0993 | -0.410523 | 0.6592 | 0.4702 | -0.3363 | -0.3401 | -0.3401
2 | 0.03125 | 5.10E+20 | 2.2935 | 9.4853147 | 0.4320 | 0.2989 | -0.5157 | -0.4786 | -0.4786
8 | 0.125 | 2.04E+21 | 6.7076 | 27.740514 | -0.2461 | 0.8303 | -0.2066 | -0.322 | -0.322

## Slide 16: TO1 mode with Jellium PBEsol
To confirm a relation between phonon frequency of TO1 mode and the concentration
We adopt a phenomenological equation from ref[1]
Our fitting
= ~ 3.1 * 10-19 meV2 cm3
Ref[1]
= ~ 1.8 * 10-19 meV2 cm3
[1] Annals of Physics 417 168107 (2020)
Jellium is good agreement for phonon
ω2(meV2)
x=1/8
(SrTi1-xNbxO3)

## Slide 17: Tight Binding model for STO
E - Efermi (eV)
= t2g orbital of Ti
Γ X|Γ Y|Γ Z|Γ S|Γ T|Γ U|Γ R
Band structure of STO
t2
t1
t3
x
y
Only t2g orbital considered for Tight Binding(TB)
t1, t2 and t3 are hopping parameters

## Slide 18: Tight binding model with phonon displacement
Self energy : e1 (for dxy) e2 (for dyz , dxz)
TB parameters for t2g of Ti
+ d ∙ uTO1 =
Distorted unit-cell by phonon mode
uTO1 : eigenvector of TO1 mode
d : displacement
Γ X|Γ Y|Γ Z|Γ S|Γ T|Γ U|Γ R
DFT
TB
Energy
Band structure of distorted STO
t2
t1
t3
x
y
xyz | hopping | d orbital | xyz | hopping | d orbital
R001 | t1' | xz | R011 | - | xz
 | t2 | xy |  | - | xy
 | t1' | yz |  | t3' | yz
R100 | t1'' | xz | R101 | t3' | xz
 | t1 | xy |  | - | xy
 | t2' | yz |  | - | yz
R010 | t2' | xz | R110 | - | xz
 | t1 | xy |  | t3 | xy
 | t1'' | yz |  | - | yz

## Slide 19: Energy splitting by symmetry breaking by TO1 displacement
Γ
R
-R
(0,0,0)
(0.5,0.5,0.5)
ΔE
where k=kx=ky=kz
ΔE
ΔE
K-space
Fit to get

## Slide 20: TB parameters with phonon displacement
d (Å)
TB parameter
d (Å)
x | n | 
0 | 0.000E+00 | 검
0.000156 | 2.644E+18 | 갈
0.001563 | 2.644E+19 | 빨
0.003125 | 5.288E+19 | 주
0.007813 | 1.322E+20 | 노

## Slide 21: Dipole with doping effect
x | n | 
0 | 0.00E+00 | 검
0.000156 | 2.55E+18 | 갈
0.001563 | 2.55E+19 | 빨
0.003125 | 5.10E+19 | 주
0.007813 | 1.27E+20 | 노
0.015625 | 2.55E+20 | 초
0.03125 | 5.10E+20 | 파
0.125 | 2.04E+21 | 보
dipole
Set Ti [0,0,0]
Dipole = ∑ ( ∆chg * r)
- Dis : 0 – 0.13 & n : 0 – 1.27E+20
구간에서 도핑이 증가하면 dipole이 감소
- Dipole 감소하면 > 복원력 감소 > 진동수 감소
d (Å)

## Slide 22: Conclusions
Using DFT, we calculate SrTiO3 with jellium model to describe Nb-doped SrTiO3.
Phonon is well described with jellium model.
Electronic band structure has tiny change with jellium model.
Dipole results show good agreement with phonon frequency.
To do
nnn hopping? Ti – O interaction?
- quantitative analysis for dipole and phonon

## Slide 23: Computational details
Vienna Ab-initio Simulation Package (VASP)
Exchange-correlation energy functional : PBEsol
The kinetic energy cutoff : 600 eV
Hellmann–Feynman force : 0.01 eV/Å.
Monkhorst–Pack scheme for k-point sampling
  6 × 6 × 6 for band structures, 3 × 3 × 3 for phonon calculation with 4 × 4 × 4 supercell
Full-relativistic SOC was considered using the noncollinear formalism as implemented in VASP